Q40 Fencing & Gates Specification

To be read in conjunction with Preliminaries/General conditions

Description: 		Perimeter security fencing panel system with timber infills

Standard: 		BS1722-14: 2017

BS EN ISO 1461:2009

BS EN 13438:2013

Manufacturer: 		CLD Fencing Systems   Info@cld-systems.com

Tel. 01270 764751 www.cld-systems.com

Product Reference:	CLD Exempla Timber Panel System

Panel type:	Profiled mesh panel system with timber infills. Number of profiles varies according to height.

Panel width:	2505mm

Wire diameter:	5mm nominal

Mesh size:	200 x 55mm

Available heights

Select as required 	2 profiles: 630mm, 830mm, 1030mm, 1230mm

3 profiles: 1530mm, 1730mm, 1930mm

4 profiles: 2330mm, 2530mm, 2730mm

5 profiles: 3030mm only

Nominal heights:	0.6m to 3.0m

Finish: 	Polyester powder-coated to 60-80 microns or 160-200 microns with marine grade and metallics. Any RAL colour available

Top edge projection:	30mm

Panel installation:	Bottom of panel approx 40mm above ground

Security topping	n/a

options:

Posts: 	RHS, galvanised after manufacture and polyester powder-coated to match fencing

Post dimensions:	Minimum 60mm x 40mm

Maximum post

Centres:		2515mm

Fixings: 			41mm x 21mm clamping channels and CLD SafeTFix hidden fixing system

Foundations: 		Set posts in holes minimum 300mm diameter x 800mm deep.

Note: Contractor/client is responsible for the foundation size suitable for the ground conditions and fence height.

Warranty: 	Mesh: Minimum of 15 years against manufacturing defects. Weave: minimum 2 years guarantee, against colour fading

Notes:	All dimensions are nominal, for further information please contact CLD Fencing Systems.

Information is correct at time of production. As part of our policy of continuous improvement, we reserve the right to alter product specification without notice.